## Slide 1
Real-time TDDFT
for extremely nonlinear and ultrafast phenomena
Shunsuke A. Sato
1. Center for Computational Sciences, University of Tsukuba, Japan
2. Max Planck Institute for the Structure and Dynamics of Matter, Hamburg

## Slide 2
Introduction to extremely nonlinear and ultrafast phenomena
Attosecond science for solids
Intense and fs laser pulses induce nonlinear ultrafast phenomena in solids.
Agustin Schiffrin, et al, Nature 493,70 (2013)
Opt-electronic device
about 500nm
To understand the microscopic mechanism of such strongly-nonlinear ultrafast phenomena in solids.
For this aim, we employ the first-principles calculation based on
time-dependent density functional theory (TDDFT).
Our research aim

## Slide 3
Time-dependent Kohn-Sham equation for solids
Time-dependent Kohn-Sham equation with uniform electric fields in the length gauge
Gauge transformation
Time-dependent Kohn-Sham equation with uniform electric fields in the velocigy gauge
Bloch theorem

## Slide 4
How to solve the TDKS equations
We employ real-time and real-space method.
Real-scape method (Finite-difference method in space)
Real-time method (Finite-difference method in time)
We usually employ 4th order Taylor expansion method.
Yabana group@Japan
http://salmon-tddft.jp

## Slide 5
Input
Laser fields
Laser polarization
Electric current
Output
Electron dynamics calculation (RT-TDDFT)
Electron density in Si
Laser pulse
Bulk Si
Si atoms

## Slide 6
Real-time TDDFT simulation
Input
Output
Maxwell equation
Input
Output
Polarization
(for isolated systems)
Current (Polarization) is a functional of , and it can be computed with RT-TDDFT simulation!

## Slide 7
Expansion of current
If a system has a translational symmetry in time:
First order (linear) response
Second order response

## Slide 8
Linear response
for
Causality
Fourier transform
Optical conductivity
Fourier transform

## Slide 9
Dielectric function of Si
(Becke-Jonson meta-GGA is used)
Electric current under the distortion
Application of TDDFT to linear response
calculate electron dynamics under a small distortion, .
1st step:
evaluate electric current, , as a function of time.
2nd step:
3rd step:
evaluate optical properties by Fourier analysis:
How to evaluate dielectric function with RT-TDDFT
Silicon

## Slide 10
Nonlinear response (Nonlinear optics)
2nd order nonlinear current
Second harmonic generation
Photovoltaic effect

## Slide 11
“ Ironically, the faint spot did not appear in the figure in Physical Review Letters because someone at the printing company thought it was a blemish and erased it, says Weinreich.”
First observation of nonlinear optical (Second harmonic generation)
P. A. Franken, A. E. Hill, C. W. Peters, and G. Weinreich, Phys. Rev. Lett. 7, 118 (1961)
https://physics.aps.org/articles/v7/112
David Lindley, Physics 7, 112

## Slide 12
Nonlinear response (Nonlinear optics) from RT-TDDFT simulation

## Slide 13
Nonlinear response (Nonlinear optics) from RT-TDDFT simulation
M. Uemoto, et al., J. Chem. Phys. 150, 094101 (2019)
(a.u.)
(a.u.)
Application to diamond
Laser parameters:
Photon energy = 1.55 eV
Pulse duration = 16 fs
We compute the polarization:

## Slide 14
Nonlinear response (Nonlinear optics) from RT-TDDFT simulation
M. Uemoto, et al., J. Chem. Phys. 150, 094101 (2019)
(a.u.)
(a.u.)
Response of diamond

## Slide 15
We can conduct pump-probe experiments with the first-principles calculation.
Numerical pump-probe experiments
calculating electron dynamics under pump and probe pulses.
evaluate electric current as a function of time
Electric field
1st step:
2nd step:
evaluate optical properties by Fourier analysis:
3rd step:
Electric current
S.A.S. et al, Phys. Rev. B 89, 064304 (2014).

## Slide 16
Dielectric function of laser-excited silicon
The dielectric function shows metallic behavior due to photo-excited carrier
Ground state
W/cm2
W/cm2
W/cm2
Drude model
S.A.S. et al, Phys. Rev. B 89, 064304 (2014).
Numerical pump-probe experiments

## Slide 17
Application to attosecond physics!
But before that…

## Slide 18
Laser-induced Intra-band transition and inter-band transition
Inter-band transition
- Photo-absorption semiconductor
Intra-band transition
- Origin of metallic current
- Bloch oscillation
electron

## Slide 19
Attosecond transient absorption spectroscopy (GaAs)
The experiments were done in Prof. Keller’s experimental group@ETH Zurich
Experimental setup
Material: 100nm GaAs thinfilm
Pump-pulse: 5fs IR pulse ( eV)
Probe-pulse: 250as XUV ( eV)
F. Schlaepfer, et al, Nature Physics 14, 560 (2018).
Bnad gap: 1.42 eV

## Slide 20
Attosecond transient absorption spectroscopy (GaAs)
(arb. unit)
Delay (fs)
Experiment

## Slide 21
Reference calculation w/o pump
Numerical pump-probe experiments
Input
Output
Pump-probe calculation
Input
Output
Theory

## Slide 22
Attosecond transient absorption spectroscopy (GaAs)
(arb. unit)
Delay (fs)
Experiment
Theory
So nice!
But, do we need theory?

## Slide 23
Towards microscopic understanding
Photon energy (eV)
Time delay (fs)
Orbital decomposition analysis
Theoretical signal
Electronic structure of GaAs
As-3d to valence bands
As-3d to conduction bands

## Slide 24
Orbital decomposition analysis
Photon energy (eV)
Time delay (fs)
Probe Hamiltonian decomposition
As-3d to valence
As-3d to conduction

## Slide 25
Towards microscopic understanding
Photon energy (eV)
Time delay (fs)
Orbital decomposition analysis
Theoretical signal
Electronic structure of GaAs
As-3d to valence bands
As-3d to conduction bands

## Slide 26
Transition from As-3d to conduction bands
Inter-band
Intra-band
Intra-band
Valence band
Conduction band
E
k
As-3d band
Parabolic 3-band model
Photon energy (ev)
Theoretical signal (As-3d to conduction)
(arb. Unit)
Fishbone structure!
Conduction bottom
Electronic structure of GaAs

## Slide 27
27
3-band model
Intra-band only (3-band model)
Inter-band only (3-band model)
Transition from As-3d to conduction bands
First-principle
Photon energy [eV]

## Slide 28
Summary of microscopic interpretation (GaAs)
Experiment
Theory
Inter-band
Intra-band
Intra-band
Transition from As-3d to valence and conduction bands is dominant.
Long-lasting signal originates from the electron (hole) created by the pump (inter-band transition).
Transient signal originates from the IR-induced intra-band transition.
Intra-band transition can be dominant even in the resonant condition, where the pump photon-energy matches to the band gap.
F. Schlaepfer, et al, Nature Physics 14, 560 (2018).

## Slide 29
Summary
RT-TDDFT simulation can be seen a machinery to evaluate the current/polarization as a functional of electric fields:
The computed current/polarization contains all orders of the nonlinear contributions in addition to the linear response. Hence, by analyzing the results of RT-TDDFT simulation, one can evaluate all order of linear/nonlinear optical properties of systems.
I introduced a numerical pump-probe scheme which mimics the real-experimental scheme with RT-TDDFT simulations for applications of ultrafast phenomena and nonequilibrium physics.
The TDDFT simulation can:
Be directly comparable with experimental results.
Provide microscopic insights into phenomena.
Make a bridge between experiments and simplified models for further understanding.
Take-home messages (more general?)
Take-home messages

## Slide 30
Thank you for your attention!!
And, enjoy the school & workshop!!