## Slide 1
Spin Supersolid on a Triangular Lattice:
A Tensor Network Study of a Cobalt-based Quantum Magnet
Yuan Gao
Beihang U & Institute of Theoretical Physics
2026.02
Entanglement and topology in interacting quantum matter
Wei Li
ITP

## Slide 2: Outline
1. Introduction of spin supersolid
2. Thermal tensor network
XTRG, tanTRG, stoMPS, …
3. Spin supersolid state in triangular lattice antiferromagnet Na2BaCo(PO4)2
Model determination, phase diagram, magnetocaloric effect, …
4. Spin dynamics of spin supersolid state
Goldstone mode, pseudo-Goldstone mode, roton mode, …
5. Spin Seebeck effect of triangular lattice spin supersolid
Imaginary-time approximation for spin current, spin supercurrent, …

## Slide 3: States of Matter: Solid, Superfluid, and More ...
U(1) Phase symmetry breaking
→ Superfluid order
Solid
Superfluid
Translation symmetry breaking
→ Crystal structure

## Slide 4: Can a Solid Be “Superfluid”?
A. J. Leggett
PRL 25, 1543 (1970)
Nonclassical rotational inertia (NCRI):
2003 Nobel physics
superfluid fraction
Kim et al., Nature 427, 225 (2004)

## Slide 5: Can a Solid Be “Superfluid”?
A. J. Leggett
PRL 25, 1543 (1970)
Nonclassical rotational inertia (NCRI):
2003 Nobel physics
superfluid fraction
PRL 109, 155301 (2012)
Absence of Supersolidity

## Slide 6: Supersolid Phase of Hard-Core Bosons
PRL 95, 237204 (2005)
Hard-core boson model
Solid order: lattice translation symmetry breaking
Superfluid order: U(1) gauge symmetry breaking

## Slide 7: Spin Analog of Supersolid: Spin Supersolid
Hard-core boson to spin 1/2
Hard-core boson
Spin model
Spin realization of supersolid in hard-core boson——Spin supersolid

## Slide 8: Exotic magnetic state in Triangular Lattice Antiferromagnet
The magnetic field induces a wealth of spin states
Sellmann et al., Phys. Rev. B 91, 081104 (2015)
Phase diagram of triangular lattice Heisenberg model under magnetic field
Yamamoto et al., Phys. Rev. B 100, 140410(R) (2019)
Out-of-plane field
In-plane field
Supersolid Y
Supersolid V

## Slide 9: Exotic magnetic state in Triangular Lattice Antiferromagnet
Zhu et al., Phys. Rev. Lett. 120, 207203 (2018)
Highly competition of magnetic order and quantum spin liquid
Bond-dependent interaction
Next-nearest neighbor interaction
Hu et al., Phys. Rev. B 92, 140403(R) (2015)
Phase diagram of triangular lattice extended Heisenberg model

## Slide 10: Triangular Lattice Spin Supersolid
Supersolid ground state (Y state)
Triangular lattice Heisenberg model with easy-axis anisotropic
Out-of-plane projection:
Solid order
In-plane projection:
Superfluid order
Is there a quantum magnetic material realization?

## Slide 11: Triangular Lattice Antiferromagnet : Na2BaCo(PO4)2
Lattice structure of Na2BaCo(PO4)2
Building block: effective spin-1/2
Co2+ forms effective spin-1/2 under the crystal electric field and spin orbit coupling
Zhong et. al., PNAS 116, 14505 (2019)

## Slide 12: Triangular Lattice Antiferromagnet : Na2BaCo(PO4)2
Intra-plane charge density landscape
Building block: effective spin-1/2
Co2+ forms effective spin-1/2 under the crystal electric field and spin orbit coupling
There exists super-super exchange interaction between Co2+ , forming a perfect triangular lattice structure
Gao, et al., npj Quantum Materials (2022)

## Slide 13: Experimental Result of Na2BaCo(PO4)2
Specific heat measurement
Inelastic neutron scattering
Zhong et al., Proc. Natl. Acad. Sci. 116 (29) 14505-14510 (2019)
Strong spin fluctuations
No phase transition down to 300 mK

## Slide 14: Experimental Result of Na2BaCo(PO4)2
Specific heat measurement
Inelastic neutron scattering
Strong spin fluctuations
Phase transition at 150 mK?
Li, et al., Nature Commun. 11, 4216 (2020).

## Slide 15: Experimental Result of Na2BaCo(PO4)2
Specific heat measurement
Inelastic neutron scattering
Quantum spin liquid or magnetic order state?

## Slide 16
Thermal tensor network

## Slide 17: Tensor Network State
Tensor network representation
Matrix product operator
Density matrix
L
W
Exponential wall in many-body system
Tensor network for quantum many-body system
Thermal tensor network
Numerical renormalization group
Density matrix renormalization group
2D tensor network state: iPEPS
Density Matrix RG
S. White, 1992 PRL milestone

## Slide 18: Thermal Tensor Network
Exponential tensor renormalization group (XTRG):
Chen, et al., PRX 8, 031082 (2018)

## Slide 19: Thermal Tensor Network
Haegeman, et al., PRL 107, 070601 (2011)
Li, et al., PRL 130, 226502 (2023)
Imaginary-time evolution of the density matrix by time-dependent variational principle
Tangent space tensor renormalization group (tanTRG):
https://github.com/ThermoTN/
Qiaoyi Li
ITP (on the market)

## Slide 20
Spin supersolid state in triangular lattice antiferromagnet Na2BaCo(PO4)2
Sizhuo Yu, Yuan Gao, Bin-Bin Chen, and Wei Li, Chinese Phys. Lett. 38 097502 (2021)
Yuan Gao, […], Yuan Wan, and Wei Li, npj Quantum Materials 7, 89 (2022)
Junsen Xiang, Chuandi Zhang, Yuan Gao, […], Wentao Jin, Wei Li, Peijie Sun, and Gang Su, Nature 625, 270 (2024)
Wei Li
ITP
Gang Su
ITP
Yuan Wan
IOP

## Slide 21: Model Determination: Symmetry Analysis
Site symmetry of Co:
  3-fold rotation w.r.t c-axis
  2-fold rotation w.r.t a-axis
  Inversion
Site symmetry of Co-Co center: 2/m
  2-fold rotation w.r.t a-axis
  Inversion
Gao et. al., npj Quantum Materials 7, 89 (2022)

## Slide 22: Model Determination: Bayesian Optimization
Yu et. al., Chinese Phys. Lett. 38 097502 (2021)
Automatic parameter research
Loss function
Parameter space

## Slide 23: Effective Model of Na2BaCo(PO4)2
The 20 best sets among 450 iterations
Landscape of loss function
Negligible off-diagonal terms
Single solution

## Slide 24: Effective Model of Na2BaCo(PO4)2
The 20 best sets among 450 iterations
Landscape of loss function

## Slide 25: Effective Model of Na2BaCo(PO4)2
Zero-field specific heat and magnetic susceptibility
Ground state magnetization

## Slide 26: Ground-State Phase diagram
Out-of-plane magnetic field
Comparison with neutron diffraction
Exp.
DMRG
Xiang et. al., Nature 625, 270 (2024)
Wentao Jin
BUAA

## Slide 27: Finite-Temperature Phase Diagram
Classical Mento Carlo simulation
Spin supersolid phase
Zero Field
Out-of-plane: 6-fold degenerate ground state
  2 BKT transitions with emergent U(1)
In-plane: U(1) symmetry breaking
  BKT transition
High field
  Potts + BKT or one phase transition?

## Slide 28: Finite-Temperature Phase Diagram
tanTRG result
Experiment
Excellent agreement between experimental and theoretical results!

## Slide 29: Finite-Temperature Phase Diagram
Spin stiffness
Huang et. al., arxiv:2509.03489 (2025)

## Slide 30: Finite-Temperature Phase Diagram
Spin stiffness
Experiment
Huang et. al., arxiv:2509.03489 (2025)

## Slide 31: Giant Magnetocaloric Effect of Spin Supersolid
Supersolid
Adiabatic demagnetization curve
Spin supersolid refrigeration achieves an extremely low temperature of 94 mK!
The experimental measurements are highly consistent with theoretical calculations, providing further evidence for spin supersolid.
Xiang et. al., Nature 625, 270(2024)
Peijie Sun
IOP
Junsen Xiang
IOP
94 mK

## Slide 32: Giant Magnetocaloric Effect of Spin Supersolid
Grüneisen ratio
The peak value is 4 times more than that of general coolants
—— Giant MCE in spin supersolid
Differential characterization of the MCE
Xiang et. al., Nature 625, 270(2024)

## Slide 33
Spin dynamics of spin supersolid state
Yuan Gao, Chuandi Zhang, […], Wentao Jin, Gang Su, and Wei Li PRB 110, 214408 (2024)
Wentao Jin
BUAA

## Slide 34: Tensor Network Approach for Spin Dynamics
Real-time correlation function
DMRG

## Slide 35: Tensor Network Approach for Spin Dynamics
Real-time correlation function
TDVP

## Slide 36: Tensor Network Approach for Spin Dynamics
Dynamical spin structure factor
Spectral function
Real-time correlation function

## Slide 37: Tensor Network Approach for Spin Dynamics
Dynamical spin structure factor
Spectral function
Real-time correlation function
In practice
Parzen window function

## Slide 38: Comparison with Inelastic Neutron Scattering Result
Gapless Goldstone mode at K point
Microscopic evidence of spin supersolid state existence
Gao et al., PRB 110, 214408 (2024)

## Slide 39: Spin Excitations of Spin SuperSolid
Spin resolved spectral function
In-plane spin dynamics
Out-of-plane spin dynamics

## Slide 40: Goldstone Mode and Pseudo-Goldstone Mode
Goldstone mode
Pseudo-Goldstone mode
Spin superfluidity
Spin solidity

## Slide 41: Origin of The Pseudo-Goldstone Mode
Classical energy of Y state
Net magnetization: accidental degenerate
Linear spin-wave result
Two Goldstone mode

## Slide 42: Origin of The Pseudo-Goldstone Mode
Classical energy of Y state
Net magnetization: accidental degenerate
Complex order parameter
Energy landscape of quantum spin supersolid
6-fold anisotropic Mexican-hat
Quantum fluctuations break the accidental degenerate and induce the Pseudo-Goldstone modes.

## Slide 43: Spin Excitations of Spin SuperSolid
Double magnon-roton excitations
Magnetic analog of phonon-roton dispersion in superfluid helium
Goldstone mode
Pseudo-Goldstone mode

## Slide 44: Spin Supersolid in K2Co(SeO3)2
Observation of Goldstone mode, pseudo-Goldstone mode and roton mode
Chen et al., arxiv:2402.15869 (2024)
Zhu et al., PRL 133, 186704 (2024)
Zhu et al., npj quantum materials 10, 74 (2025)

## Slide 45: Spin Supersolid and Quantum Spin Liquid
Mean-field calculations
DMRG phase diagram
Gallegos et al., PRL 134, 196702 (2025)
Jia et al., PRR 6, 033031 (2024)

## Slide 46
Spin Seebeck Effect of Triangular-lattice Spin Supersolid
What is the macroscopic quantum phenomenon for spin supersolid?
Sadamichi Maekawa
Riken
Yuan Gao, Yixuan Huang, Sadamichi Maekawa, and Wei Li, PRL 135, 236504 (2025)

## Slide 47: Spin Seebeck Effect in a Magnetic Insulator

## Slide 48: Linear-Response Theory of Spin Seebeck Effect
: temperature of the magnet (spin)
: temperature of the metal
: magnetic field along direction
Experimental setup:

## Slide 49: Linear-Response Theory of Spin Seebeck Effect
Total Hamiltonian
weak coupling

## Slide 50: Linear-Response Theory of Spin Seebeck Effect
Spin current (via non-equilibrium GF method)
How to calculate the normalized spin current ?
Spin-wave theory for ordered magnets, what about disordered spin systems?

## Slide 51: Imaginary-time Approximation for Normalized Spin Current
Spin current
Real-time spin dynamics:
: temperature of the magnet (spin)
: temperature of the metal
: magnetic field along direction
Imaginary time correlation:
with .

## Slide 52: Imaginary-time Approximation for Normalized Spin Current
We assume is analytical near , i.e.
At low temperature, we have
Real-time formula
Imaginary-time formula
Compare these two formulas, we arrive at:

## Slide 53: Thermal Tensor Network Approach
Tensor-network simulations of the spin Seebeck effect
Imaginary-time correlation function:

## Slide 54
Benchmarks on Heisenberg spin chain

## Slide 55: Experimental Observation of Spinon Spin Current
Sign reversal of spin current

## Slide 56: Spin Current in 1D Heisenberg Spin Chain
Heisenberg spin-chain Hamiltonian
Sign reversal: consistent with experimental result
Algebraic scaling of negative spinon spin current in Tomonaga-Luttinger liquid (TLL)
Universal scaling of spin current @ QCP

## Slide 57: Benchmarks on 1D Heisenberg Spin Chain
ITA captures the sign reversal in spin current
Excellent agreement in low-T scaling behaviors between and
Heisenberg spin-chain Hamiltonian
Finite-temperature spin dynamics

## Slide 58: Benchmarks on 1D Heisenberg Spin Chain
Hirobe et al., Nature Phys 13, 30 (2017)
ITA captures the sign reversal in spin current
Excellent agreement in low-T scaling behaviors between and
Heisenberg spin-chain Hamiltonian

## Slide 59
Spin Seebeck effect of Triangular Spin Supersolid

## Slide 60: Spin current of Spin Supersolid State
Easy-axis XXZ Hamiltonian of Na2BaCo(PO4)2
Supersolid phase diagram
Supersolid Y (SSY)
Up-up-down (UUD)
Supersolid V (SSV)
Polarized state (PL)
Sign reversal: detect the phase boundary of spin supersolid phases
W=6 cylinder

## Slide 61: Linear spin wave theory for SSE
Spin current behaviors in supersolid phase lies beyond LSWT!
Quantum many-body calculation
Linear spin wave theory

## Slide 62: Direction of Spin Current
Spin current
-dM/dT

## Slide 63: SSE as a Probe of QCPs
Spin current with constant temperature
Spin current at constant magnetic field
Identify QCPs from peaks and dips
Universal temperature scaling of spin current at QCPs

## Slide 64: Universal Scaling of SSE at QCPs
Spin current at U(1)-symmetric polarization quantum critical points
Spin current
At the polarization QCPs
Universal scaling of spin current

## Slide 65: Spin Supercurrent in Spin Supersolid
Non-zero spin current survives even at the zero-temperature limit.
Persistent spin current in spin supersolid state

## Slide 66: Spin Supercurrent in Spin Supersolid
Momentum resolved spin current
Goldstone-mode-mediated spin transport
Non-zero spin current survives even at the zero-temperature limit.
Persistent spin current in spin supersolid state

## Slide 67: Spin Supercurrent in Spin Supersolid
Two key predictions: (I) Sign Reversal (II) Persistent spin supercurrent
Recall Leggett’s renowned proposal
non-classical rotational inertia
normal
non-classical
Persistent spin current in spin supersolid state
1. Rotate the solid in an annulus below the transition temperature and detect the effective moment of inertia.
2. Rotate the solid above the critical angular velocity and then bring the container to rest.
Experimental probe

## Slide 68: Summary
Thermal tensor network for quantum magnet
Effective model for Na2BaCo(PO4)2: Nearly ideal easy-axis XXZ model with spin supersolid
Giant magnetocaloric effect: New pathway to sub-Kelvin cooling
Spin excitations of spin supersolid: Goldstone mode, pseudo-Goldstone mode, and roton mode
Spin Supercurrent: Macroscopic quantum transport phenomenon in spin supersolid

## Slide 69
Thanks for your attention!